## Slide 1
Virus Based Materials
20.109 Spring 2017

## Slide 2
Using Bacteriophage, or “phage”
A virus that infects bacteria
A Combinatorial Approach…..
Gene 3
insertion
Peptide Insert Expressed
on Protein 3
Protein
Coat
Gene
(New England BioLabs)

## Slide 3
M13 bacteriophage
Images created by Steven Kottman, published in Science (2004) 303, 213
2,700 copies of pVIII coat proteins
~ 6.5 nm
~ 900 nm
ssDNA

## Slide 4: Construction of p8 library
-
+
ori
lacZ α
M13SK
viral vector
gVIII
gIII
p8 inserts
Double cut DNA
Digestion
+
Ligation
and
……
Transformation
Recombinant
Recombinant
……
5’-Gnm (nnm)6 nnG-3’
3’-A CGT Cnm (nnm)6 nnC CTA G -5’

## Slide 5: Peptide Libraries & Selection
Science, 296, 891,2002
Science, 303, 213, 2004
Science, 312,885, 2006
Science , 324,1051, 2009
Substrate Screening
Washing
Amplification
Repeat
http://www.spectrum.ieee.org/WEBONLY/publicfeature/nov03/1103bio.html#f3
Phage Library
Nature,405, 665, 2000
Nature Materials,4,496 2005
Nature Materials, 5,234,2006
Nature Nanotechnology, 2010
Nature Nanotechnology, 2011
Nature Nanotechnology, 2012
Nature Communications, 2013
Nature Communications, 2014
Nature Materials, 2015
Substrates:
Semiconductors
Insulators
Metals
Magnetic Materials
Conducting polymers
CNTs

## Slide 6: Schematic Diagram for Gold Nanowire
Gold ions
  Incubated with p8#9
  Partly reduced by ascorbic acid
  Formation of nanowires in static condition with silver catalyst
  (VSGSSPDS) Chung-Yi Chiang
Youjin Lee

## Slide 7
TEM Images of Gold nm Nanowires
Relatively uniform diameter along the length 10,15, 20, 25, 30, 50 nm

## Slide 8
From
DNA
to Device

## Slide 9: Energy Storage: Lithium ion battery
= Li+
= LiPF6
Charged state
Li6C (graphite anode)
Li2O/Coo (cobalt oxide anode)
Anode
Cathode
FePO4 cathode
CoO2 cathode
e-
e-
C (graphite anode)
Co3O4 (cobalt oxide anode)
LiFePO4 cathode
LiCoO2 cathode
Discharged state
Discharging

## Slide 10: Portable Battery Applications
Battery Requirement:
High energy density
High power
Light weight
Flexible

## Slide 11: Batteries: Concept and Principle
Main components:
  Anode or negative electrode
  Cathode or positive electrode
  Electrolyte – flow of ions
Battery is a storage device which converts chemical energy into electrical energy

## Slide 12: Operation of a cell
Discharge:
  When cell is connected to an external load, electrons flow from the anode, which is oxidized, through the external load to the cathode, where the electrons are accepted and the cathode material is reduced.
  The electric circuit is completed in the electrolyte by the flow of anions (negative ions) and cations (positive ions) to the anode and cathode, respectively.

## Slide 13: Cathode vs Anode
Negative electrode, oxidation, loss of electron
Positive electrode, cathodic reaction, gain of electron
Li Li+ + e-
Cu2+ + 2e- Cu

## Slide 14: Theoretical Voltage
The standard potential of the cell is determined by the type pf the active materials (cathode and anode) in the cell.

## Slide 15: Theoretical Capacity
Theoretical capacity of a cell is determined by the amount of active materials in the cell.
Theoretical capacity is the total quantity of electricity involved in the electrochemical reactions (in terms of coulombs or ampere-hours).
  1 gram-equivalent weight of material deliver 96,485 C or 26.8 Ah. (Farday Constant, magnitude of electric charge per mole of electrons)
Theoretical capacity for Zn (Molecular Weight 65.4 g)
Zn2+ (aq)+ 2e- Zn (S)

## Slide 16: Cathode and Anode design consideration
Choose electrode materials with:
  High standard potential difference
  Fast reactions at electrodes
  High capacity
  Stable electrodes
  lightweight

## Slide 17: Operation of a Cell
Useful delivered voltage by a cell is reduced by:
  IR drop
    Due to the internal impedance of a cell
  Polarization
At what operating conditions a cell can deliver most of the theoretical available energy?
Cell Polarization as a function of operating current (Linden’s Handbooks of Batteries)

## Slide 18: Lemon Battery
Making a battery with a lemon, penny and galvanized nail (Zn-coated) as the electrodes
  Negative electrode?
  Positive electrode?
  Why do we need the lemon?
  What if we use 2 pennies?
Zn2+ (aq)+ 2e- Zn (S) -0.76(v)
Cu2+ (aq)+ 2e- Cu (S) 0.34 (v)

## Slide 19: Battery Metrics
Energy Density: Energy stored in a cell
Wh/kg (Gravimetric)
Wh/L (Volumetric)
Capacity: Amount of charge stored
ie. gravimetric capacity in mAh/g
C-Rate: Is a measure of a rate at which a battery is discharged relative to its maximum capacity.
1C means that the discharge current will discharge the entire battery in 1 hour.
Charge or discharge rate C/X
X = # hours to (dis)charge
X. Ma et al. J. Electrochem.Soc. 157 8 A925-A931 (2010)

## Slide 20: Classifications of Cells and Batteries
Primary cells
Not capable of being recharged electrically
Good shelf life,
high energy density at low to moderate discharge rate,
No or little maintenance
Ease of use
Secondary or rechargeable cells
Can be recharged electrically
High power density
High discharge rate
Flat discharge curve
Good low temperature performance
Reserve batteries
Primary type
long term storage
Fuel cells
Active material are fed into the cell from an external source
Capable of producing electrical energy as long as the active materials are fed to the electrodes

## Slide 21: Battery Performance-Upper limits of Energy Density
Chart: Electrical Energy storage (Wh/kg)
| 1946.0 | 1955.0 | 1965.0 | 1985.0 | 1995.0 | 1940.0 | 1955.0 | 1985.0 | 2000.0
Primary Batteries | 40 | 50 | 90 | 140 | 210
Secondary Batteris | 35 | 35 | 90 | 160

## Slide 22: Batteries and Fuels
Chart: Energy Density (Wh/Kg)
| 1940.0 | 1955.0 | 1985.0 | 2005.0
Rechargeable Batteries | 35 | 45 | 80 | 160
Rechargeable Batteries:
High power density
High discharge rate
Flat discharge curve
Good low temperature performance
Chart: Energy Density (Wh/Kg)
| Li-Ion | Gasoline
Series 1 | 150
Series 2 | 1200
1 Wh/kg ~ 1 mile diving range

## Slide 23: Lithium ion Batteries (LIBs)
LIBs are comprised of cells that employ lithium intercalation compounds as the positive and negative electrodes
Li Li++ e-
Li++ e-+ LixCoO2 Li1+xCoO2
Li++ e-+ Co4+ Li++Co3+

## Slide 24: LIBs: Possibilities and Challenges
LIB electrode materials requirements:
Reversibly incorporate Lithium without structural change
High redox potential between anode and cathode
Incorporate large quantities of lithium
High lithium ion diffusivity
Good electronic conductivity
Prepared from inexpensive reagents
Low cost synthesis
Capacities of common Li-ion electrode materials. Chem. Mater. 2014, 26.

## Slide 25: How to Improve the State of the Art?
Solutions:
Nano-structuring the functional materials
  Increasing surface to volume ratio
Increasing the electronic conductivity by integrating conductive additives
    Creating percolating network
Problems:
Ion diffusivity
Electronic conductivity

## Slide 26: Studying Bio-templated Materials for LIBs for the First Time
Yun Jung Lee et al., Science (2009)
The Bio-cathode materials with SWCNT on the tail of the virus.
  Improved energy density
  Imporved power density

## Slide 27: Bio-Enabled Energy Storage on a Continuum of Scales
Li-O2
(12,000 Wh/kg Theor.)
Grid and Microgrid
Power Density Limited
Cost and Portability Limited
Electric Ground Vehicles
Unmanned Aerial Vehicles
Wearable Electronics
Virus-Templated Metal Nanofoams
Biotemplated Sodium-Ion Batteries
Lithium and Sodium Sulfur Batteries
Flow Batteries
Lithium-Oxygen,
Sodium-Oxygen,
Sulfur-Based Cathodes,
Sodium Intercalation,
Carbon Nanotube/Active Material Bio-enabled Composites
Electrospun Interpenetrating Battery Cloths
Below: Electrospun polymer matte
Above: Raven UAV
Below Left: Virus-templated Nickel current collector
Below Right: “Robobee”
Ma, Science, 2013
Small Scale
Large Scale

## Slide 28
Science, 312, 885-888, 2006
Kitae Nam
Paula Hammond, Yet-Ming Chiang

## Slide 29
Generation 1 Virus Based Battery Virus - Co3O4 Anode
1st Cycle irreversibility due to additives
Cobalt coated Virus in solution state
Cu
Separator + Electrolyte (LiPF6)
Co3O4 virus
Li
Anodes grown and assembled
in flask by virus !
Virus based anode
wires placed on Cu
Initial Gen 1
cycling (vs. Li) shows all of the virus- produced Co3O4 is electrochem. active
Theor. capacity for
stoichiometric rxn
with 8 Li per Co3O4
commercial
Reversible Capacity : 600 to 750 mAh/g
about 2 times higher than carbon based anode

## Slide 30
Engineered M13 viruses for the hybrid Au-Co3O4 nanowire
Au-specific peptide selection using phage display library
Genetic engineering with plasmid system
Amplification
Peptide library
Elution
Au nanoparticle can be attached with this motif
Gold binding peptide sequence:
LKAHLPPSRLPS
Notes: Gold nanoparticles were chosen based on their ability to provide high electronic conductivity where needed, the ability to maintain a thermodynamically stable interface with Co3O4, and the potential to act as a chemical catalyst for electrochemical reactions at the nanoscale. We designed a bifunctional virus template that simultaneously expressed two different peptide motifs.
To improve this further, we again turned to genetic engineering. While keeping the genetic code for the cobalt assembly, we added an additional strand of DNA that produces virus proteins that bind to gold. Therefore, two types of protein were fused around the virus as shown in Figure 3. The viruses then assembled as nanowires composed of both cobalt oxide and gold particles. The resulting electrodes stored 30 percent more energy than the pure cobalt oxide version.

## Slide 31
Genetic Modification Produces New Hybrid Anodes for Increased Capacity Au-Co3O4 Nanowire
Gold nanoparticles bound on the virus
Cobalt oxide nucleation & growth
Has gene to grow co oxide and gene to bind gold
Notes: After removing excess unbound gold nanoparticles by centrifugation, Co3O4 was nucleated and grown via the tetra-glutamate functionality, resulting in hybrid nanostructures of 5 nm Au nanoparticles spatially interspersed within the Co3O4 wires

## Slide 32
Polymer
Virus
Battery
Material
Virus mediated nanobattery components
Transmission Electron Microscope Images
Virus enabled assembly
of nanostructured battery
Atomic Force Microscope Images

## Slide 33: Genetically Engineered High Power Battery by Encoding Multiple Genes
Yun Jung Lee Hyunjung Yi, Gerd Ceder , Michael Strano
Science , 324,1051, 2009

## Slide 34: Virus Binding Carbon Nanotubes

## Slide 35
Electrons from the current collector can transport along SWNT “highway” networks percolating throughout the electrodes transferring energy in a very short time.
Genetically Engineered High Power Cathode
-

## Slide 36
High power performance scales with the binding affinity of p3 toward SWNTs.
Stable capacity retention reflects structural stability of hybrid nanostructures.
1 C
Electrochemical Properties of a-FePO4 Viral Nanowires

## Slide 38
http://www.dsjournal.com/armyseeksheud.html
Li air batteries
900 Wh kg-1
Li ion batteries
~250 Wh kg-1
Current limitations for
Li-air electrodes
Large overpotential
Low current density
Cycle life
Cost efficiency
Bruce, P. G. et al. Nature Materials (2011)