# Text boxes

Project 1

5/4/2016 4:31:01 PM

Comment:

Spectrum processing : Red

No peaks omitted

Quantitation method : Cliff Lorimer thin ratio section.

Processing option : All elements analyzed (Normalised)

Number of iterations = 1

Standardless

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| C K | 35.93 | 57.75 |  |
| O K | 19.21 | 23.17 |  |
| Na K | 3.90 | 3.27 |  |
| Mg K | 0.34 | 0.27 |  |
| Si K | 0.25 | 0.17 |  |
| P K | 6.15 | 3.84 |  |
| S K | 0.22 | 0.13 |  |
| Cl K | 0.63 | 0.34 |  |
| K K | 1.27 | 0.63 |  |
| Ca K | 1.24 | 0.60 |  |
| Fe K | 12.43 | 4.30 |  |
| Cu K | 18.12 | 5.50 |  |
| Au L | 0.31 | 0.03 |  |
| Totals | 100.00 |  |  |

Project 1

5/4/2016 4:31:20 PM

Comment:

Spectrum processing : Purple

No peaks omitted

Quantitation method : Cliff Lorimer thin ratio section.

Processing option : All elements analyzed (Normalised)

Number of iterations = 1

Standardless

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| C K | 52.77 | 76.14 |  |
| O K | 8.52 | 9.22 |  |
| Na K | 3.14 | 2.37 |  |
| Mg K | 0.39 | 0.28 |  |
| Si K | 0.44 | 0.27 |  |
| P K | 4.40 | 2.46 |  |
| S K | 0.36 | 0.19 |  |
| Cl K | 0.64 | 0.31 |  |
| K K | 0.52 | 0.23 |  |
| Ca K | 2.26 | 0.98 |  |
| Fe K | 8.32 | 2.58 |  |
| Cu K | 18.14 | 4.95 |  |
| Au L | 0.12 | 0.01 |  |
| Totals | 100.00 |  |  |

Project 1

5/4/2016 4:31:45 PM

Comment:

Spectrum processing : Orange

No peaks omitted

Quantitation method : Cliff Lorimer thin ratio section.

Processing option : All elements analyzed (Normalised)

Number of iterations = 1

Standardless

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| C K | 41.67 | 68.22 |  |
| O K | 12.93 | 15.89 |  |
| Si K | 1.35 | 0.95 |  |
| P K | 4.09 | 2.60 |  |
| Cl K | 0.14 | 0.08 |  |
| K K | 0.37 | 0.19 |  |
| Ca K | 1.43 | 0.70 |  |
| Fe K | 8.69 | 3.06 |  |
| Cu K | 25.75 | 7.97 |  |
| Au L | 3.57 | 0.36 |  |
| Totals | 100.00 |  |  |

Project 1

5/4/2016 4:32:05 PM

Comment:

Spectrum processing : Pink

No peaks omitted

Quantitation method : Cliff Lorimer thin ratio section.

Processing option : All elements analyzed (Normalised)

Number of iterations = 1

Standardless

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| C K | 24.09 | 42.65 |  |
| O K | 25.20 | 33.50 |  |
| Na K | 2.97 | 2.75 |  |
| Si K | 0.69 | 0.52 |  |
| P K | 9.20 | 6.31 |  |
| Cl K | 0.80 | 0.48 |  |
| K K | 1.59 | 0.86 |  |
| Ca K | 1.79 | 0.95 |  |
| Fe K | 17.79 | 6.78 |  |
| Cu K | 15.37 | 5.14 |  |
| Au L | 0.52 | 0.06 |  |
| Totals | 100.00 |  |  |

Project 1

5/4/2016 4:32:19 PM

Comment:

Spectrum processing : Blue

No peaks omitted

Quantitation method : Cliff Lorimer thin ratio section.

Processing option : All elements analyzed (Normalised)

Number of iterations = 1

Standardless

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| C K | 28.80 | 55.01 |  |
| O K | 15.96 | 22.88 |  |
| P K | 6.80 | 5.04 |  |
| Cl K | 0.38 | 0.24 |  |
| K K | 0.78 | 0.46 |  |
| Ca K | 1.34 | 0.77 |  |
| Fe K | 13.30 | 5.46 |  |
| Cu K | 25.88 | 9.34 |  |
| Au L | 6.75 | 0.79 |  |
| Totals | 100.00 |  |  |